[image: image1.jpg]


[image: image2.jpg]STA]N GUA.RD FABRIC PROTECTION




HIGH PERFORMANCE ECO-FABRIC FOR VERTICAL SURFACES
Wallcoverings ( Panel Systems ( Partitions 

T
reated with Stain Guard. Stain Guard’s soil and stain resistance adds years to the life of a fabric. It dramatically cuts on-site maintenance and replacement costs, making every installation a better investment for your customers.
GARDEN GATE
SPECIFICATIONS
    CONTENT
       
     BACKING
        FINISH
       WEIGHT            WIDTH
    ROLL SIZE

  · 53% polyester  
  
     acrylic latex
      Stain Guard     
            14 oz.
              54"
         50 yards  


  · 47% olefin




    47% RECYCLED CONTENT 
  · 47% post-industrial
    FLAMMABILITY
  
     ABRASION RESISTANCE

COLOR FASTNESS TO LIGHT

     Class A / ASTM E-84

               (ASTM D-4157-02)



   (AATCC-16A)


     Passes: UBC 8-2

             51,000  double rubs 


         exceeds Class 4.0 / 40 hrs. 
     FS:  20    /    SD:  50
   

     Passes: Cal 117

     Passes: Vertical Burn

ENVIRONMENTAL

   does not contain:



conserving natural resources:
     

     · pvc 





  · diverts waste from landfills

    

     · chlorene




  · offsets the need to refine new crude oil

     

     · plasticizers




  · requires less energy to produce

     

     · heavy metals

     

     · formaldehyde

     

     · ozone depleting substances 

     

     · volatile organic chemicals (voc’s)



















© Hytex Industries, Inc. 2016 All rights reserved.























