[image: image1.png]$ CRYPTON.

wall




HIGH PERFORMANCE ECO-FABRIC FOR VERTICAL SURFACES
Wallcoverings ( Panel Systems ( Partitions 

U

tilizing a combination of pre-consumer and post-consumer recycled polyester to create unique performance yarns, Hytex Industries introduces our newest collection of vertical surface textiles for the commercial market.
RIVIERA
SPECIFICATIONS
    CONTENT
       
     BACKING
        FINISH
       WEIGHT            WIDTH
    ROLL SIZE

  · 100% polyester  
     acrylic latex
    CryptonWall( ‘Green’     16 oz.
              54"
         50 yards  


  




        Soil & Stain

     85 % RECYCLED CONTENT           
                          Repellant

  · 30% post-consumer


        






  · 55% post-industrial

          

    FLAMMABILITY
  
     ABRASION RESISTANCE

COLOR FASTNESS TO LIGHT

     Passes: UBC 8-2 Corner Burn
               (ASTM D-4157-02)



   (AATCC-16A)


     Class A / ASTM E-84

             100,000 double rubs 


Class 5.0 / 40 hrs. 
     FS:  25    /    SD:  25
   

     Passes: Cal 117

     Passes: Vertical Burn

ENVIRONMENTAL

   does not contain:



conserving natural resources:
     

     · pvc 





  · diverts waste from landfills

    

     · chlorene




  · offsets the need to refine new crude oil

     

     · plasticizers




  · requires less energy to produce

     

     · heavy metals

     

     · formaldehyde



Greenguard Gold Certified
     

     · ozone depleting substances 


  · Number 23850-410

     

     · volatile organic chemicals (voc’s)

  · formerly Children & Schools Gold Certified








  · meets Calif 1350 High Performance Schools
[image: image2.emf]












© Hytex Industries, Inc. 2016 All rights reserved.





©2016 CRYPTON, Inc. CRYPTON and the planet logo are registered trademarks


of CRYPTON, Inc. U.S. patent 5,565,265 and other U.S. and global patents


issued and pending.





REPREVE is a registered trademark of Unifi, Inc.














