[image: image1.png]$ CRYPTON.

wall




HIGH PERFORMANCE ECO-FABRIC FOR VERTICAL SURFACES

Wallcoverings ( Panel Systems ( Partitions 

U

tilizing a combination of pre-consumer and post-consumer recycled polyester to create unique performance yarns, Hytex Industries introduces our newest collection of vertical surface textiles for the commercial market.
TEMPO
SPECIFICATIONS
    CONTENT
       
     BACKING
        FINISH
       WEIGHT            WIDTH
    ROLL SIZE

  · 80% polyester  
    
    acrylic latex
    CryptonWall( ‘Green’     14 oz.
              54"
         50 yards  


  · 20% olefin



        Soil & Stain






  




          Repellant

     46% RECYCLED CONTENT 
  · 11% post-consumer (polyester)

          

  · 35% post-industrial (15% polyester, 20% olefin)
    FLAMMABILITY
  
     ABRASION RESISTANCE

COLOR FASTNESS TO LIGHT

     Passes: UBC 8-2 Corner Burn
               (ASTM D-4157-02)



   (AATCC-16A)


     Class A / ASTM E-84

             100,000 double rubs 

               Class 5.0 / 40 hrs. 
   

     FS:  20    /    SD:  50

     Passes: Cal 117

     Passes: Vertical Burn

ENVIRONMENTAL

      does not contain:



conserving natural resources:
     

     · pvc 





  · diverts waste from landfills

    

     · chlorene




  · offsets the need to refine new crude oil

     

     · plasticizers




  · requires less energy to produce

     

     · heavy metals

     

     · formaldehyde



Greenguard Gold Certified
     

     · ozone depleting substances 


  · Number 23850-410

     

     · volatile organic chemicals (voc’s)

  · formerly Children & Schools Gold Certified








  · meets Calif 1350 High Performance Schools
[image: image2.emf]












© Hytex Industries, Inc. 2016 All rights reserved.





©2016 CRYPTON, Inc. CRYPTON and the planet logo are registered trademarks


of CRYPTON, Inc. U.S. patent 5,565,265 and other U.S. and global patents


issued and pending.





REPREVE is a registered trademark of Unifi, Inc.














