-OEM-

   NEW MILLENIUM                                      WHISPERTEX COLLECTION
COPPERSMITH – PLISSE’

ENVIRONMENTAL SOUND CONTROL FABRICS
Vertical Surfaces ( Ceiling Systems ( Acoustical Panels

A

dimensional fabric which offers excellent acoustical properties, unmatched fade resistance, and a fire/smoke retardant Class A rating.  WhisperTex is lightweight, inexpensive, and as easy to install as conventional wallcoverings.  It is moisture resistant, mildew, rot, and bacteria resistant, and is non-allergenic.  With a commitment to the environment, we manufacture WhisperTex using post-consumer recycled materials and it is fully 100% recyclable.

SPECIFICATIONS


CONTENT
BACKING
  WEIGHT
  WIDTH

ROLL SIZE
  FLAMMABILITY

             FOSSFIBRE®
   Radiant      13 ounces/lineal yard
      54"

     50 yds.         Passes UBC 8-2/ NFPA 265

        100% Solution dyed
    fusion






              Class A / ASTM E-84

      polyester staple fiber


WhisperTex has been tested for toxicity in accordance with the Pittsburgh Protocol

       and is no more toxic than wood (LA50 method).  New York City MEA Registration #276-90M.

THICKNESS





      Coppersmith

.060"










(+/- .015")





      Plissé


.080"

TEST RESULTS

	
	
	
	

	          ASTM E-84
	  Flame Spread Rate
	    Fuel Contributed
	    Smoke Developed

	         Tunnel Test
	                15
	                  15
	                 20

	

	

	    NOTE:  The numerical flame spread rating and other test results referenced herein are not intended 

                  to reflect hazards presented by this or any other material under actual fire conditions.

	
	
	

	
	
	

	                     NRC:
	        MOISTURE REGAIN
	COLOR FASTNESS TO CROCKING

	             (ASTM C-423)
	          (ASTM D-2654)
	                   (AATCC - 8)

	    .60 over acoustical board
	                   .03%
	  Dry - Excellent, Wet - Excellent

	     .05 over gypsum board
	
	

	
	
	

	                    COLOR FASTNESS TO LIGHT
	                        ABRASION RESISTANCE

	                                  (AATCC - 16A)
	                           (ASTM D - 3597 MOD)

	                                      100 hours
	                           Voluntary Prod. TS198

	
	                      Full Commercial Serviceability

	
	
	

	
	Installation and maintenance instructions are enclosed with every WhisperTex shipment and should be carefully read prior to installation.  For best results, it is recommended that a qualified textile wallcovering installer be employed.


	


