
[image: image1.jpg]/]
FOSSHIELD



[image: image2.wmf]eco-A.R.T.
Cobblestone
ACOUSTIC RECYCLED TEXTILE
Wallcoverings ( Panels ( Exhibits ( Partitions
A dimensional fabric produced with post-consumer recycled fiber offering exceptional performance, unmatched fade resistance, and a fire/smoke retardant Class A rating.  It is lightweight and easy to install and maintain.  

eco-A.R.T. is moisture resistant, mildew, rot, and bacteria resistant and is nonallergenic.

( eco-fi® Polyester staple fiber.  High strength fibers which
(  UL classification:  Only Hytex needlepunch acoustical
   are resistant to shrinking and stretching. Highly durable.
    fabrics carry the UL label.
   100% recycled content from water & soda bottles.  

(  Passes NFPA 265 Corner
Burn Test. It is the
standard
   

   Averages 90% post-consumer content.


    test method for evaluating room fire growth contribution

(  Easy to clean and maintain.



    of Textile Wallcovering.
(  Fiber does not absorb moisture.



(  Solution dyed. Resists sun, fading - colors are fast
(  Acoustical qualities:  NRC ratings   .25  (ASTM C423)     
                   to most destructive agents.
(  Velcro compatible, pill resistant.



USAGE AREAS

DESIGNERS
HEALTH CARE
    HOSPITALITY    CORPORATE    INSTITUTIONAL    ENTERTAINMENT

(Commercial
   (Retirement
        (Ball Rooms
           (Executive
      (Schools(Auditorium)
        (Theatres

    Interiors
       Facilities
        (Conference
          Conference
          (Government &
      (Recreational

     Market
(Nursing Homes
             Rooms
             Rooms
     Mass Trans. Buildings
           Centers



     (Hospitals
   (Meeting Rooms
     (General Offices       (Day Care Centers


( Nursing Stations
Acoustical Panels ( Tack Boards ( Elevators ( Ceiling Tiles ( Office Partitions ( Chair Rails

SPECIFICATIONS
    CONTENT
       BACKING

WEIGHT
 WIDTH

ROLL SIZE
FLAMMABILITY

           eco-fi®
        Fused Poly
    24 ounces / face weight          54"
   
    33 yards
  Passes NFPA 265

 Post-Consumer Recycled







                 Class A/ASTM E-84  

 Solution Dyed Polyester

    Staple Fiber

              NRC

MOISTURE REGAIN
 COLORFASTNESS TO LIGHT     ABRASION RESISTANCE

         (ASTM C-423)
       (ASTM D-2654)
                  (AATCC-16A)


   (ASTM D-4158)
                  .25 
  

  .5%

             Class 5 - 100 hours 

             Voluntary Prod. TS198
       over gypsum board







       Full Commercial Serviceability
Fosshield® Antimicrobial Technology – silver & copper ions are incorporated into the polyester fiber and naturally attack microbes.  Fosshield® inhibits the growth of bacteria, mold and fungus, providing permanent protection.  Ions bind to any microbes that may be present on the fiber and disable their critical functions (metabolism, respirations, and reproduction).  Typical examples of microbes of common concern are Methicillin-resistant Staphylococcus aureus (MRSA), the Human rhinovirus (common cold), Steptococcus pyogenes (strep), Legionella pneumophilia (Legionaires disease), Human Coronavirus (SARS surrogate), and Feline Calicivirus (Norwalk virus).  Fosshield® is the technology incorporated into the FDA cleared SpectraShield® 9500 N95 surgical respirator mask.  In the FDA testing, Fosshield® began microbe prevention immediately and eliminated 99.99% of certain odor-causing bacteria after one hour of contact with the respirator surface.
[image: image3.png]




UNDERWRITERS LABORATORIES INC.

  
CLASSIFIED WALLCOVERING SURFACE BURNING CHARACTERISTICS

[image: image4.png]



Applied to inorganic reinforced cement board with Sairmix-7 super duty

high temperature mortar at an application rate of 55 square feet per gallon

Flame Spread 


Smoke Developed
         15



             85

NOTE:  The numerical flame spread rating and other test results referenced herein
are not intended to reflect hazards presented by this or any other material under actual fire conditions.

Installation and maintenance instructions are enclosed with every eco-A.R.T. shipment and should be carefully read

prior to installation.  For best results, it is recommended that a qualified textile wallcovering installer be employed.

�





�





�





�








Hytex Industries, Inc. – 58 York Ave. – Randolph, MA 02368 – (781) 963-4400 – www.hytex.com 

