
[image: image2]

WHISPERTEX

ENVIRONMENTAL SOUND CONTROL FABRICS

Vertical Surfaces ( Ceiling Systems ( Acoustical Panels

A

dimensional fabric which offers excellent acoustical properties, unmatched fade resistance, and a fire/smoke retardant Class A rating.  WhisperTex is lightweight, inexpensive, and as easy to install as conventional wallcoverings.  It is moisture resistant, mildew, rot, and bacteria resistant, and is non-allergenic.  With a commitment to the environment, we manufacture WhisperTex using post-consumer recycled materials and it is fully 100% recyclable.

SPECIFICATIONS


  CONTENT
BACKING
 WEIGHT
    WIDTH        ROLL SIZE
            FLAMMABILITY

                   eco-fi®
  Radiant        13 ounces/lineal yard
       54"                50 yds.         Passes UBC 8-2/ NFPA 265

            Polyester Fiber 
   Fusion






          Class A / ASTM E-84

       100% post-consumer

      recycled plastic bottles

Wallcovering ( Acoustical Panels ( Tack Boards ( Ceiling Tiles ( Office Partitions
THICKNESS





      Coppersmith

.060"










(+/- .015")





      Plissé


.080"











TEST RESULTS
	          ASTM E-84
	   Flame Spread Rate
	    Fuel Contributed
	    Smoke Developed

	         Tunnel Test
	                15
	                  15
	                 20

	

	    NOTE:  The numerical flame spread rating and other test results referenced herein are not intended 

                  to reflect hazards presented by this or any other material under actual fire conditions.

	
	
	

	                     NRC:
	        MOISTURE REGAIN
	COLOR FASTNESS TO CROCKING

	             (ASTM C-423)
	          (ASTM D-2654)
	                   (AATCC - 8)

	    .60 over acoustical board
	                   .03%
	  Dry - Excellent, Wet - Excellent

	     .05 over gypsum board
	
	

	
	
	

	                    COLOR FASTNESS TO LIGHT
	                        ABRASION RESISTANCE

	                                  (AATCC - 16A)
	                           (ASTM D - 3597 MOD)

	                                      100 hours
	                           Voluntary Prod. TS198

	
	                      Full Commercial Serviceability

	
	
	

	
	Installation and maintenance instructions are enclosed with every WhisperTex shipment and should be carefully read prior to installation.  For best results, it is recommended that a qualified textile wallcovering installer be employed.
	







































            

[image: image1]
[image: image2][image: image3.png]ad

PET



[image: image4.png]ecofi



